## Slide 1
ICAMT 2024
INTERNATIONAL
CONFERENCE
ON ADVANCED MATERIALS AND TECHNOLOGY
Hanoi, Vietnam, October 09-12, 2024
POSTER CODE: A-XXX
INVESTIGATE THE PROPERTIES OF ZN2SNO4 MATERIALS AT DIFFERENT HYDROTHERMAL
TEMPERATURES FOR GAS SENSOR APPLICATION
Nguyen Hong Hanh, Lai Van Duy, Hoang Xuan Thanh, Nguyen Duc Hoa* International Training Institute for Materials Science (ITIMS), Hanoi University of Science and Technology, No. 1, Dai Co Viet, Hai Ba Trung, Hanoi, Viet Nam.
*corresponding email : ndhoa@itims.edu.vn
EXPERIMENTAL
Investigate the properties of Zn2SnO4 material at different hydrothermal temperatures: 180oC/24h, 200oC/24h, 220oC/24h.
SEM, XRD measurement.
H2S Sensing Properties of Zn2SnO4 material at different hydrothermal temperatures.
RESULTS AND DISCUSSIONS
Fig.1, it is observed the SEM images of Zn2SnO4 material with different hydrothermal temperatures: (a) 180oC/24h; (b) 200oC/24h; (c) 220oC/24h to demonstrate the Zn2SnO4 material are nanoparticles.
In the Fig. 2, the XRD images of Zn2SnO4 material. It demonstrate all 3 samples are Zn2SnO4 material. Especially, the 200oC/24h sample with all pic are (311), (400), (511), (440), (622), (731) compare with Zn2SnO4 XRD standard.
In Fig. 3, 4, 5, we show the H2S-sensing characteristics of Zn2SnO4 at different hydrothermal temperatures: 180oC/24h, 200oC/24h, 220oC/24h were measured at different temperatures 350oC, 400oC, 450oC, under different H2S concentration from 1 ppm to 20 ppm. It showed that, the highest sensor response (S) at 400oC with H2S concentration from 5 ppm to 20 ppm.
Fig. 1. The SEM images of the synthesized Zn2SnO4.
CONCLUSIONS
INTRODUCTION
Motivation
Investigate the properties of Zn2SnO4 materials at different hydrothermal temperatures
Applied Zn2SnO4 on gas sensor
Measure the H2S-sensing characteristics of Zn2SnO4 at different hydrothermal temperatures
By investigation the properties of Zn2SnO4 material at different hydrothermal temperatures: 180oC/24h, 200oC/24h, 220oC/24h. We showed that Zn2SnO4 was the good material for the gas sensor applications.
High electron mobility
Good uniformity
High electrical conductivity
Zn2SnO4 material
Fig. 3. H2S-sensing characteristics of Zn2SnO4 at 180oC/24h hydrothermal measured at different temperatures 350oC, 400oC, 450oC : (a) transient resistance and sensor response versus time upon exposure to different H2S concentrations, (b) sensor response as a function of H2S concentrations.
(a)
(b)
(a)
180 oC / 24 h
(b)
200 oC / 24 h
(c)
220 oC / 24 h
Fig. 2. The XRD images of the synthesized Zn2SnO4.
(a)
(b)
(c)
Fig. 4. Sensor response as a function of H2S concentrations 350oC, 400oC, 450oC with (a) 200oC/24h hydrothermal (ZTO_2), 220oC/24h hydrothermal (ZTO_3).
Fig. 5. Sensor response as a function of H2S concentrations at 400oC with 180oC/24h hydrothermal (ZTO_1), 200oC/24h hydrothermal (ZTO_2), 220oC/24h hydrothermal (ZTO_3).
(a)
(b)
Acknowledgment: This research was supported by the .......................................................................................................................................
Poster size: A0